Library of Basic Inorganic Structure Types for ATOMS

GENERAL.  Most drawings are shown in clinographic orientation, rotated somewhat from a view down the a-axis.  Radii are usually about half the standard ionic or covalent radii, or one-quarter the interatomic distance.  The boundary used for the drawing is shown in yellow, and the unit cell is drawn in white, entirely in front of the structure.

BCC.STR  Body-centered cubic.  Space group Im3m.  Each atom is coordinated by 8 others, instead of 12 as in closest-packing.

CCP.STR  Cubic-closest-packed.  Space group Fm3m.  In this view the [111] direction is vertical, showing the horizontal layers of atoms.

CCP2.STR  Cubic-closest-packed.  This shows the three different layers in red, green and yellow in a hexagonal space group. See CCP.STR for the true symmetry.

CSCL.STR  Cesium chloride, CsCl.  Space group Pm3m. Each atom is coordinated by 8 atoms of the other type.

DIAMOND.STR Diamond.  Space group Fd3m. Each atom is coordinated by 4 others.

FLUORITE.STR CaF2.  Space group Fm3m.  Ca atoms are coordinated by 8 F atoms, and F atoms are coordinated by 4 Ca atoms

HCP.STR  Hexagonal-closest packed.  Space group P63/mmc.  This shows the true symmetry with all atoms alike.  In this particular structure, zinc, the bond interatomic distances between layers are greater than those within layers, so it is not ideal closes-packing.

HCP2.STR  Hexagonal-closest packed.  In a reduced symmetry, this shows the two different layers in red and green.  See HCP.STR for the true symmetry.

HEMA.STR  Hematite, Fe2O3, or corundum Al2O3.  Space group R-3c.  The oxygen atoms are in approximate hexagonal closest packing, with Fe atoms in octahedral interstices.  Because the Fe octahedra share faces, there is considerable distortion from ideal hcp.

NACL.STR  Sodium chloride, NaCl.  Space group Fm3m. Each atom is coordinated by 6 of the other kind.

NIAS.STR  Nickel arsenide (niccolite), NiAs.  Space group P63/mmc. Each atoms is coordinated by 6 of the other type.

PEROV.STR Perovskite, CaTiO3.  Space group Pm3m.  This is an idealized structure; perovskite itself has lower symmetry.  Ca atoms replace O atoms in a ccp arrangement and Ti atoms are in selected octahedal interstices.

RUTILE.STR Rutile, TiO2.  Space group P42/mnm.  TiO6 octahedra share edges to form chains in the c-axis direction, and the chains are also cross-linked in the same way.  This shows a ball-and-stick model.

RUTILEP.STR Rutile, TiO2. This shows TiO6 octahedra.

SPHALER.STR Sphalerite, ZnS.  Space group F-43m.  Each atom is coordinated by 4 of the other type.  Each type of atom forms a cubic-closest-packed arrangement. See wurzite

SPINEL.STR Spinel, MgAl2O4.  Space group Fd3m.  This ball-and-stick model has the [111] direction vertical to show the approximately ccp oxygens (horizontal).  Mg atoms are in tetrahedral interstices, and Al in octahedral interstices

SPINELP.STR Spinel, MgAl2O4.  Space group Fd3m.  This view, in standard orientation (c-axis vertical) shows AlO6 octahedra and MgO4 polyhedra

WURZITE.STR Wurzite, ZnS.  Space group P63mc.  Each atom is coordinated by 4 of the other type.  Each type of atom forms a hexagonal-closest-packed arrangement.  See sphalerite